## Slide 1
Free X-ray Diffraction software for handling at least some of the drudgery in powder diffraction analysis.
L.M.D. Cranswick
Neutron Program for Materials Research (NPMR),
National Research Council of Canada (NRC),
Building 459, Station 18, Chalk River Laboratories,
Chalk River, Ontario, Canada, K0J 1J0
E-mail: lachlan.cranswick@nrc.gc.ca
WWW: http://neutron.nrc.gc.ca/

## Slide 2
Talk Notes on the web
Via the CCP14 website:
http://www.ccp14.ac.uk/poster-talks/axaa2005/

## Slide 3
Why bother knowing about a variety of MODERN software?
Path of Most Resistance?
Using a variety of “state-of-the-art” tools can improve versatility by allowing different pathways and approaches to tackle crystallographic problems.

## Slide 4
Using the right crystallographic method can make the difference!
Using Le Bail fitting / Rietveld
Using Traditional UNIT CELL refinement Methods

## Slide 5: Talk Agenda
Start from Data conversion and phase identification
Go through to photo realistically rendering crystal structures
Via stops including
  Peak profiling
  Powder indexing
  Powder unit cell refinement
  Rietveld structure refinement (briefly as this is covered in other talks)
  Quantitative Phase Analysis (very briefly as covered in other talks)
  Photorealistic rendering of crystal structures

## Slide 6: Phase Identification/Search Match for Powder Diffraction
Two main parts to perform computer based search-match:
  1. Have a Powder Diffraction Database (buy or make your own)
  2. Search-match software that uses the above database to search
Databases:
  ICDD has the commercial powder diffraction database area sewn up http://www.icdd.com/
Nearly all Search-match programs are commercial
Refer to, "Available Search-Match Software" for a list of known software:
  http://www.ccp14.ac.uk/solution/search-match.htm
  Free Software: Brian Toby's "Portable Logic Program" (UNIX) and "MacDiff" for Apple Mac freeware by Rainer Petschick

## Slide 7: Phase Identification/Search Match for Powder Diffraction 2 of 3 Identifying an organic – DL-Valine

## Slide 8: Phase Identification/Search Match for Powder Diffraction 3 of 3 Multiphase mixture: Flourite, Corundum, Zincite

## Slide 9: Sample Preparation and Data Collection
  Assumption is that you know about appropriate sample preparation and data collection
  However, many hardware vendors might not provide the required flexibility in data collection

## Slide 10: Variable Count Time data collection
Main idea here is to increase the raw intensity of selected peak areas to assist in the “required” analysis:
  Up till now, if at all, mainly done for refinement (e.g., Hill and Madsen method)
On point detector (e.g., Bragg Bretano flat plate system), do this by varying the count time in a pre-defined manner
  (Can also provide more time effective counting time)
Fixed Count Time
Variable Count Time

## Slide 11
Variable Count Time applications
Equally relevant to problems where you need to adequately profile fit small / trace peaks which might not be significantly above background in a “routine”, time effective fixed count time data collection - e.g.,;
  Powder Indexing
  Unit Cell refinement
  Quantitative Rietveld Analysis

## Slide 12: VCT to aid in profile fitting (1 of 3) Fixed Count Time

## Slide 13: VCT to aid in profile fitting (2 of 3) Variable Count Time

## Slide 14: VCT to aid in profile fitting (3 of 3) Overlaying VCT and FCT

## Slide 15
Where is VCT Data Collection?
Not a routine or available option in commercial XRD control software (with the exception of Bede Scientific)
Something to keep an eye on - or request from vendors.

## Slide 16: Has the structure been solved already? Crystallographic Structure Databases
ICSD (Inorganics)
  http://www.fiz-karlsruhe.de/
  Web accessible demonstration (4% of the database):
    http://barns.ill.fr/dif/icsd/
MDF/CRYSTMET
  (Metals and Alloys)
  http://www.tothcanada.com/
CCSD (organics and organometallics)
  (Organics and Organometallics)
  http://www.ccdc.cam.ac.uk/

## Slide 17: ICSD via the Web
Using an Interface created by Alan Hewat
There is a trend for databases to use the web due to the convenience and effectiveness. Also has advantage of being operating system independent for users.
  http://icsd.ill.fr/icsd/

## Slide 18: Powder Data Conversion / Importing Data
Initial problem in powder diffraction can be getting the data in the right format. For interconverting powder diffraction data: a variety of programs exist which in combination can pretty much get you from one format to another
Summary list of available software: http://www.ccp14.ac.uk/solution/powderdataconv/
Text Editors may occassionally be required: converting UNIX ACSII to DOS ASCII, getting rid of spaces or tabs , column editing:
Freeware PFE Editor for Windows:
  http://www.lancs.ac.uk/people/cpaap/pfe/
Freeware ConTEXT Editor for Windows (does column editing)
  http://www.context.cx/
Example of ConvX for Windows by Mark Bowden - Mass data powder diffraction data converter

## Slide 19: Structure Importing, Conversion and Transformation
Summary list of available software at: http://www.ccp14.ac.uk/solution/structconv/
Be careful to check the results
Crystallographic knowledge is require for custom operations - pre and post transformation translations, etc
Best program for the moment is the “shareware” Cryscon
  http://www.shapesoftware.com/#anchor_cryscon
Example of Cryscon for Windows by Eric Dowty

## Slide 20: Powder Diffraction Utility Software
Examining Data, peak finding, background stripping, alpha-2 stripping
Powder v 2.00: http://www.ccp14.ac.uk/tutorial/powder/
Powder X, http://www.ccp14.ac.uk/tutorial/powderx/
WinFIT,
  http://www.geol.uni-erlangen.de/html/software/soft.html
Winplotr, http://www-llb.cea.fr/winplotr/winplotr.htm
XFIT, http://www.ccp14.ac.uk/tutorial/xfit-95/xfit.htm
WinPLOTR
(data display, peak find, peak profiling, indexing)

## Slide 21: Peak Profiling (indexing, unit cell refinement, size/strain, etc)
For Overall Summary of available peak profiling software refer to:
http://www.ccp14.ac.uk/solution/peakprofiling/
These include: CMPR, DRXWin, EFLECH, GPLSFT, pearson.xls, SHADOW, Powder v2.00, PowderX, Winfit, Winplotr, XFIT
Examples of XFIT for Windows

## Slide 22: Powder Indexing - a non trivial endeavour
For Overall Summary of available powder indexing software refer to:
http://www.ccp14.ac.uk/solution/indexing/
Powder Indexing: Autox, Ito, Dicvol, Treor, Taup/Powder, Lzon, Losh, Kohl, Scanix, Xrayscan, EFLECH/Index, Supercell
Linking Suites: Crysfire, Powder v2.00, PowderX, PROSZKI, WinPlotr, Chekcell
supercel is a specialise indexing program by Juan Rodriguez-Carvajal for indexing Super Cell and Incommensurate cells. (available within Winplotr)
http://www-llb.cea.fr/winplotr/winplotr.htm
ftp://bali.saclay.cea.fr/pub/divers/fullprof.2k/

## Slide 23: Powder Indexing - the “Crysfire” suite
At present the CRYSFIRE software by Robin Shirley links 9 different indexing programs (including ito, dicvol, treor, taup, kohl, lzon and fjzn) together with a common interface and using intelligent defaults. Important to have access to as many indexing programs as possible so you can get a feel for the range of possible solutions. (not free for commercial use)
http://www.ccp14.ac.uk/tutorial/crys/
Example of CRYSFIRE Screen prompting the saving into one of 9 different indexing program formats:

## Slide 24: Chekcell: Interpreting Crysfire Summary Files: Powder Indexing and Spacegroup Assignment
Crysfire interlinks with Chekcell for Windows (part of the LMGP suite for Windows by Jean Laugier and Bernard Bochu). Chekcell provides a graphical interface for manually and automatically suggesting a best cell/spacegroup combination using both FOM and algorithms relating to parsimony of superfluous HKLs.
http://www.ccp14.ac.uk/tutorial/lmgp/

## Slide 25: Other new programs (impurity peak tolerant)
DICVOL 2004 by A. Boultif & D. Louer
  http://www.ccp14.ac.uk/ccp/web-mirrors/dicvol/
McMaille reconstructed whole profile indexing by Armel Le Bail
  http://sdpd.univ-lemans.fr/McMaille/

## Slide 26: Have to Index: Really a phase ID problem
When not in the database, you may have to try and index as part of phase Identification
Following is of a herbicide commonly used in South Africa.

## Slide 27: Unit Cell Refinement
For Overall Summary of available unit cell refinement software refer to:
http://www.ccp14.ac.uk/solution/unitcellrefine/
This includes:
  Celref, LAPOD, Refcel, Unitcell, Eracel, Powder v2.00, XLAT, etc
Can be helpful to perform a conventional unit-cell refinement prior to a Le Bail fit or quantitative analysis when given cell values are far from the actual values

## Slide 28: Unit Cell Refinement - what is needed
Profiled peak positions (using a peak profile program)
Cell (and spacegroup)
UNIT Cell refinement program to perform the refinement
Useful to check the alignment of your diffractometer (don’t just rely on one Silicon or Quartz peak); perform a unit cell refinement on the entire 2-theta range supported by the diffractometer (e.g., 5 to 160 for many Bragg Brentano diffractometers)

## Slide 29: CELREF for Unit Cell Refinement
by Jean Laugier and Bernard Bochu
http://www.ccp14.ac.uk/tutorial/lmgp/

## Slide 30: Using CELREF for Unit Cell Refinement Loading the raw data file (optional)

## Slide 31: Using CELREF for Unit Cell Refinement Loading the peak listing file

## Slide 32: Using CELREF for Unit Cell Refinement Load or input the cell and spacegroup

## Slide 33: Using CELREF for Unit Cell Refinement Auto-match peak positions to HKLs

## Slide 34: Using CELREF for Unit Cell Refinement Perform the refinement

## Slide 35: UNITCell refinement with internal standard (such as NBS/NIST Silicon)
XLAT - Berhard Rupp
  ftp://jgiqc.llnl.gov/
  http://www.ccp14.ac.uk/ccp/ccp14/ftp-mirror/llnlrupp/
  ftp://ftp.ccp14.ac.uk/ccp14/ftp-mirror/llnlrupp/

## Slide 36: Full Profile Fitting (Powder)
For Overall Summary of available full profile analysis refer to:
Le Bail based: http://www.ccp14.ac.uk/solution/lebail/
Pawley Based: http://www.ccp14.ac.uk/solution/pawley/
The most common method of full profile fitting is that of Le Bail fitting: which is in most Rietveld packages. It is useful for:
  Spacegroup Assignment
  Unit Cell Refinement (especially when overlap is a problem)
  Extracting Intensities for Structure Solution

## Slide 37: Unit Cell Refinement: Mass Le Bail fitting: multi-phase - overlapping patterns
Using Le Bail fitting
Using Traditional Methods

## Slide 38: Quickly and automatically tracking changes in masses of data using a script in GSAS:

## Slide 39
Structure Refinement using Powder Diffraction Data (Rietveld Refinement)
Large range of programs to choose from:
  http://www.ccp14.ac.uk/mirror/mirror.htm
Many specialize for particular types of problems, incommensurate structures, quantitative analysis, polymers, etc.
ARITVE, BGMN, DBWS, DEBVIN, EXPO
Fullprof, GSAS, Koalariet, LHPM-Rietica, MAUD for Java (GPL’d)
Premos/Remos, ProDD, Profil, Riet7/SR5, Rietan 2000 (GPL’d)
Rietquan, Simref, WinMprof, XND, XRS-82/DLS-76

## Slide 40
Rietveld Programs - GSAS by von Dreele and Larson
With Graphical User Interface using Brian Toby’s EXPGUI
Still got to appreciate and know your crystallography for inserting and refining the crystal structure
  http://www.ccp14.ac.uk/solution/gsas/

## Slide 41: GSAS Rietveld: Some Relevant Background
by Bob von Dreele and Alan Larsen
Menu based control
Available for Windows / DOS / Linux / SGI
Separate GUI by Brian Toby (EXPGUI)
Combined X-ray / Neutron / Single Crystal / Powder Diffraction
Integrated Fourier map generation and viewing
GSAS resources, tutorials and links (including links to EXPGUI)
  http://www.ccp14.ac.uk/solution/gsas/
Restraints
  Bond angle
  Bond length
  Planar
  Total Chemistry / charge balance
  Chiral volume
  Phi/psi group
  Torsion angle
Manual Marquadt damping
Atom shift limits
Lots of other features

## Slide 42: GSAS : Combined refinement on both XRD and Neutron
X-ray 7.6% R(F**2)
(~3.8% R Bragg)
Neutron 4.2% R(F**2)
(~2.1% R Bragg)

## Slide 43: MAUD for Java : GPL’d - can be used by all!
Tutorial on “Performing an x-ray quantitative analysis in seven easy steps!”:
http://www.ing.unitn.it/~luttero/maud/tutorial/

## Slide 44: Quantitative Phase Analysis
Non-trivial and in many cases, custom solutions may be required.
Rietveld programs are commonly used for Quantitative Analysis (refer list in previous slide).
Maud for Java Quantitative Analysis Tutorial:
http://www.ing.unitn.it/~luttero/maud/tutorial/
Refer to non-Rietveld references cited in:
Following using Koalariet / XFIT
(fundamental parameters)
http://www.ccp14.ac.uk/tutorial/xfit-95/
http://www.ccp14.ac.uk/poster-talks/david-hay-quant-notes-axaa99/

## Slide 45
For trace quantitative analysis, variable count time on the trace peaks that matter could be beneficial - if your data collection software allows you to.

## Slide 46
Peak profiling on trace peaks is difficult with fixed count time! Same goes with Rietveld fitting of trace phases.

## Slide 47
Peak profiling on trace peaks can be made easier by using Variable Count time methods.

## Slide 48
“Accurate” Quantitative Phase Analysis - is it routinely easy?
Based on the IUCr CPD Quant Round Robin
(http://www.iucr.org/iucr-top/comm/cpd/QARR/)
The answer seems to be No!
A quote from Armel Le Bail’s Tmacle “twinned refinement” manual seems appropriate:
  http://sdpd.univ-lemans.fr/museum/tmacle92.zip
GOOD LUCK
IT'S VERY HARD! DON'T YOU THINK SO?
ONLY THE BOSS SAID THAT IT IS EASY,
BUT HE NEVER TRIED!
TO HAVE THE SOLUTION DEPENDS ON YOU,
NOT ON THIS PROGRAM WHICH IS JUST
ABLE TO TEST YOUR HYPOTHESIS.......

## Slide 49
Powder diffraction pattern calculation Poudrix for Windows
Powder Cell by Jean Laugier and Bernard Bochu
http://www.ccp14.ac.uk/tutorial/lmgp/#pdw
Poudrix can handle anomalous dispersion at non X-ray tube wavelengths with the option of two models:
  Brenann and Cowan
  Sasaki

## Slide 50
Powder diffraction pattern calculation Powder Cell for Windows
By Werner Kraus and Gert Nolze
http://www.ccp14.ac.uk/tutorial/powdcell/
Is freeware but if you want the software continued, consider giving a minimum of 15 Euros under an "Agreement on a Financing Contribution for Subsidy Projects"

## Slide 51
Simulating multiple phase patterns with Powder Cell
Is possible to easily load two or more phases and calculate powder patterns:
  Examine the degree of peak overlap
  Estimate number of counts required to see desired phases prior to running them
  Look at elementary effects of geometry, wavelength and peak offset

## Slide 52
Simulating multiple phase patterns with Powder Cell Open the phase / crystal structure using File Load: (in this case : anatase and rutile)

## Slide 53
Change the diffraction conditions as required using the “Diffraction, Experiment” menu

## Slide 54
At this point, what would the diffraction pattern of 1% Anatase in Rutile look like - use the “Diffraction Phase Options”

## Slide 55
Then OK to calculate the diffraction pattern of 1% Anatase in Rutile : Recalculate

## Slide 56
“Freeware” for photorealistic hardcopy output of structures GRETEP and Povray
Gretep for Windows (Jean Laugier and
Bernard Bochu)
  Can open Shelx, PowderCell, LazyPulvarix and CIF. Export Povray files.
  Point and click operation. Save all information into a Gretep file (atom labels, bond labels, colours, etc)
  http://www.ccp14.ac.uk/tutorial/lmgp/#gretep
http://www.ccp14.ac.uk/ccp/web-mirrors/lmgp-laugier-bochu/
Povray
  Freeware open source photorealistic rendering software
  http://www.povray.org

## Slide 57
GRETEP - rendered structure

## Slide 58
DrawXTL for for Windows by Larry Finger and Martin Kroeker - Structure Drawing software
http://www.lwfinger.net/drawxtl/

## Slide 59
Freeware for photorealistic hardcopy output of structures Balls and Sticks by Sung J. Kang & Tadashi C. Ozawa
http://www.toycrate.org
Individual point and click creation of polyhedra and bonds via a Windows graphical user interface

## Slide 60: Some Other Web Resources
IUCr Commission on Powder Diffraction Newsletter (free hardcopy sent by air-mail)
  http://www.iucr.org/iucr-top/comm/cpd/Newsletters/
  http://www.au.iucr.org/iucr-top/comm/cpd/Newsletters/
ICDD
  http://www.icdd.com/
IUCr News Online
  http://www.iucr.org/cww-top/crystal.index.html
  http://www.au.iucr.org/cww-top/crystal.index.html
IUCr Sincris Software Database
  http://www.se.iucr.org/sincris-top/

## Slide 61: Summary
Large Genetic Diversity of Software
This diversity is necessary to help you get the job done.
Getting better all the time (some areas faster than others)
Free available for Academics and Students and much is freely available for everyone (if in doubt check)
BUT remember that difficult problems have a habit of being difficult to do!
Much of which is downloadable via the EPSRC funded CCP14 website:
http://www.ccp14.ac.uk
E-mail: ccp14@dl.ac.uk