## Slide 1: Tricks for solving difficult structures using Sir2002
Lachlan M. D. Cranswick
Neutron Program for Materials Research (NMPR)
National Research Council of Canada (NRC)
Building 459, Station 18,
Chalk River Laboratories,
Chalk River, Ontario,
Canada, K0J 1J0
E-mail: lachlan.cranswick@nrc.gc.ca
WWW: http://neutron.nrc.gc.ca/

## Slide 2: Sir2002
Can solve structures up to and beyond 2000 non-hydrogen atoms in the asymmetric unit
Free for academics and non-profit use
Sir2002 web address:
  http://www.ic.cnr.it/
Some tricks may be required to get it to solve on some difficult structures.
All “what is Sir2002 actually doing under the hood” questions should be put on hold until members of the Sirware group arrive for the main conference.

## Slide 3: Creating a starting File
Assumption for this demonstration is you have already read up or can read up on the routine use of Sir2002. Either using the GUI or an ASCII editor
%window
%structure cyclodextrin
%init
%job cyclodextrin
%data
cell 29.420 29.891 30.686 90.000 90.000 90.000
space P 21 21 2
cont C 1000 H 800 O 400
reflections sadf.hkl
format (3i4,2f8.2)
%phase
%continue

## Slide 4: Spawning Sir2002 from WinGX
Very easy to start Sir2002 from the WinGX suite using the “Solve, Sir-2002” menu option

## Slide 5: Solving Simple Structures
Just in case more complex demonstrations go pear-shaped
Click Go button, solve structure (tetracyline hydrochloride) Clegg and Teat

## Slide 6: Exporting for viewing and refinement
Use the “File, Export” option:
  Shelx,
  Crystals,
  Xtal,
  PDB,
  Caos,
  Shakal,
  Moldraw,
  XYZ format

## Slide 7: Solving Structures with Weak Data
Using all the data, the Sir2002 defaults may not work and structure might not solve with Sir2002

## Slide 8: Solving Structures with Weak Data
Try a Rhomax cutoff (maximum Sin / that will be used) Based on WinGX defaults: Rhomax 0.250
In the control file:
%window
%structure veryfast
%init
%job veryfast in C 2/c from Crystals distribution
%data
Cell 15.610 13.121 16.353 90.000 100.623 90.000
Space C 2/c
Content C 192 H 128
Rhomax 0.250
Reflections veryfast.hkl
Format (3i4,2f8.2)
Fosquare
%continue

## Slide 9: Solving Structures with Weak Data
With Rhomax, structure now solves on the 11th Trial

## Slide 10: Sir97/Sir92 on small structures
Sir97/92 Can be very fast compared to Sir2002 on small structures – few seconds
(following using the Rhomax directive as well)

## Slide 11: Using “Relax” with “pseudotranslational effects”
If you are told there are “pseudotranslational” effects, and Sir2002 seems to be going nowhere, it can be good to try the “Relax” option.
(Following originally solved by manual interpretation of a 3D Patterson map: I.E. Grey, R.S. Roth, M.L. Balmer, Journal of Solid State Chemistry, 131, 38-42 (1997))

## Slide 12: “Relax” and pseudo effects
Under “Modify, Setup”, select “Relax”

## Slide 13: “Relax” helps to convincingly solve the structure

## Slide 14: Solving Large Structures with lots of pseudo symmetry with Sir2002
“A new octahedral tilt system in the perovskite phase Ca3Nb2O8” L.M.D. Cranswick, W.G. Mumme, I.E. Grey, R.S. Roth, and P. Bordet; Journal of Solid State Chemistry 172 (2003) 178–187
Actually solved from single crystal X-ray and powder X-ray and neutron diffraction over a duration of around 3 years using manual model building and crystal chemistry arguments.
Rhombohedral (pseudo-cubic) perovskite structure (22 B cations, 20 A cations, 56 Oxygen atoms. Total of 98 atoms. )

## Slide 15: Try 1: Using the standard SIr2002 defaults
Following is frustrating for demonstrating non-defaults, as latest Sir2002 now solves this with standard defaults.
So will go through the “non-default process”.
With defaults - solves in around 15 minutes on Trial 7 with an R factor of 20.70%
Two problems with polymeric inorganics:
  the structure has to be solved
  then you have to recognize that it has been solved – easy in hindsight – but perhaps not on the first occassion.
Using different options can lead to different “solved” structures of which one may be easier to interpret.

## Slide 16: Try 2 (if not solved) : using Relax only
Stops on Trial 4 with an R factor of 21.26% and structure is solved.

## Slide 17: Try 3 (if not solved) : using Relax and < 20% R-factor stop (default is < 25%)
Stops on Trial 17 with an R factor of 18.28%.
Structure is buildable/refinable (a few weeks/months work to refine to completion using something like Jana or Shelx)

## Slide 18: Try 4 (if not solved – or even if it did) now using Relax and < 15% R-factor stop
Stops on Trial 10 with an R factor of 20.36%.
Structure looks buildable/refinable

## Slide 19: Try 5 (if Sir2002 stopped at 20% to 25% solution) : just using < 20% R-factor stop
Goes through all 200 Trial with lowest R factor of 17.80% in Trial 95 (vs 18.28% in previous slide)

## Slide 20: Solving Large Structures
Click Go button, solve structure
Patience is a virtue – the following Cyclodextrin is expected to have around 250 atoms in the asymmetric unit and Z’=4. Takes ~20 hours to solve on 2GHz PC – on trial 132.

## Slide 21: Exploring previous Trials
Output list may show a other trials worth looking at

## Slide 22: Fourier Cycling on Trial 132
Output list may show a trial number worth looking at
To got directly to this trial, after %phase, use the command “trial 132”
%window
%structure cyclodextrin
%init
%job cyclodextrin
%data
cell 29.420 29.891 30.686 90.000 90.000 90.000
space P 21 21 2
cont C 1000 H 800 O 400
reflections sadf.hkl
format (3i4,2f8.2)
%phase
trial 132
%continue

## Slide 23: Solving on Trial 132
Immediately goes to solve on Trial 132

## Slide 24: Solving on Trial 132 – 20 minutes later
Solution from Trial 132 is now displayed

## Slide 25: Showing Trial 132 – 1 second later
If the Sir2002 Binary file (*.bin) has not been corrupted, you can immediately show the solved result for any trial.
%window
%Structure cyclodex
%Phase
Trial 132
%continue

## Slide 26: Showing Trial 132 – 1 second later
Solution from Trial 132 is now displayed
May have to leave Sir2002 to finish a round of direct space refinement (10 minutes wait in this case)

## Slide 27: Shelxd
An equivalent program to Sir2002 is Shelxd by George Sheldrick
  (was originally hoping to have a speaker talk about on Shelxd here)
Shelxd has different options to Sir2002 (via ASCII control file only – not a GUI) and can also solve merohedrally twinned single crystal data, if you have:
  Twin matrix (TWIN instruction)
  Estimate of the twin ratio (BASF parameter)
http://shelx.uni-ac.gwdg.de/SHELX/

## Slide 28: Summary
Sir2002 download:
    http://www.ic.cnr.it/
Shelxd webpage:
  http://shelx.uni-ac.gwdg.de/SHELX/