## Slide 1: Powder Indexing of Large Volume Unit Cells (including protein data) using Crysfire
Robin Shirley
School of Human Sciences
University of Surrey
Guildford, UK
Session 1b, Single Crystal and Powder Diffraction Software Workshop, ECM-21, Durban, South Africa
24 August 2003

## Slide 2: Summary
What is powder indexing and why is it needed?
Crysfire 2003 indexing example (high-quality lab data).
Indexing with Crysfire and Chekcell.
Figures of merit - classic and joint-probability.
Mountaineering in indexing’s solution space.
Crysfire 2002, Crysfire 2003 (and Industrial Crysfire).
A “buyer’s guide” for indexing programs.
How much does cell volume matter? Can one index a protein?
Crysfire 2003 protein example (Zn Insulin):
Self-calibration for 2Theta zero error;
Rescaling and indexing;
Space-group and higher symmetry: Chekcell.
Conclusions and acknowledgements.

## Slide 3
What is powder indexing and why is it needed?
Before you can get started on an ab initio powder structure, you need to know the unit cell
otherwise the intensity from each profile point can’t be located in reciprocal space, and progress is impossible.
Inferring the unit cell from the limited and partly overlapping and degraded information in a powder pattern is called powder indexing (or auto-indexing).
This is a complex process of induction that’s far beyond manual methods in all but the easiest cases.

## Slide 4
Perhaps more than for any other aspect of powder diffraction,
success in powder indexing depends critically on the resolution and accuracy of one’s observed data.
Although there are tools for correcting data with systematic errors (self-calibration example to follow).
Data Quality

## Slide 5
“Indexing? - No problem, we just use program ... [fill in your lab’s preference]”
“And does that always work?”
“Well, no - sometimes it doesn’t come out, so we drop that problem and move on.”
Indexing can be harder than actually solving the structure.
It can seem an all-or-nothing process, that either comes out painlessly or with much effort, if at all
(especially if you only have one tool in your toolbox).
Different types of pattern can need different programs.
Running Dicvol (or Treor) on a problem that needs Lzon (or Kohl) is like trying to hammer in a nail with a screwdriver.

## Slide 6: < A first look at Crysfire 2003 & Chekcell> Indexing a low-volume monoclinic lab dataset using programs in combination (Demonstration)

## Slide 7: Indexing with Crysfire + Chekcell
Crysfire starts from powder line positions (2Thetas or d-spacings) and returns with a list of plausible trial cells, sorted by number of lines indexed and figure of merit.
So it should have done the really hard work of pinning down the solution to somewhere specific in solution space.
Its work is finished when it has provided a list that contains the correct cell in some form (or a derivative cell of it).
But the solutions may be in unhelpful settings or expressed in too-low symmetry, and not say much about space groups.
Chekcell is a graphical toolkit that can help the user to identify the best crystal system and setting.
It can narrow the symmetry to a few specific spacegroups for each trial solution, and do an extended Le Page search for derivative sub- and super-cells (for one trial solution at a time).

## Slide 8: Indexing with Crysfire + Chekcell (2)
To summarise:
Crysfire does the heavy stuff that you couldn’t think of doing by hand, but doesn’t stop to polish its solutions.
Chekcell provides graphical tools to help with the polishing job, which in principle you could do by hand, but this way is much easier and faster.

## Slide 9: Classic Figures of Merit (“M20”, etc)
Indexing figures of merit (M) are roughly the inverse of R-factors, but based on differences in obs and calc Q [=1/dsq] rather than in intensity.
Different programs define M somewhat differently, but that isn’t usually important - M is too sensitive to tiny changes in cell constant for minor differences to be significant.
But it’s worth noting that no current program actually uses De Wolff’s original M20 definition for its M (though they often call it M20), because its handling of “unindexed” lines would be too cumbersome.
(IMHO) The best-conditioned and most conservative M is M1, as used by Crysfire’s CA and MM commands.
Crysfire simply records whatever each program reported.

## Slide 10: Joint-Probability Figures of Merit (Pr, Ir)
The figures of merit discussed so far all depend on the sums of discrepancies - the differences between observed and calculated line positions.
Thus they report the average misfit between observations and model, and can be severely degraded by any non-model features such as impurity lines.
Figures of merit can also be based on the joint probability of getting the observed level of fit across the pattern.
Two new joint-probability figures of merit Pr and Ir are provided in the new Hmap program in Crysfire 2003.
Unlike M20-style figures of merit, these depend mainly on the regions that fit well with that model, and are largely transparent to badly-fitting features like impurity lines.
For more about joint-probability methods, come to the indexing microsymposium on Thursday morning.

## Slide 11: Mountaineering in indexing’s solution-space
If we can specify 6 values for the cell constants (three sides and three angles), we will have fixed the unit cell.
So in that sense, indexing implies finding a point with a high figure of merit in a 6-dimensional “solution space”.
We could step-scan across this space, making a visual map of its landscape of high and low values of M (or Pr / Ir), which is what Mmap (or Hmap) does.
The next slide shows such a topographical map for a section through the solution space of an organic-metallic dyestuff, to give some idea of what they can look like.
Each peak in the map corresponds to a relatively high figure of merit, and hence a possible trial solution.

## Slide 12
M1 surface in the QD/QE (i.e. */*) section for -Cu phthalocyanine (from Powder47)

## Slide 13: Where are we now? - Crysfire 2002, Crysfire 2003 and Industrial Crysfire
The current distribution is still Crysfire 2002, but what I’m demonstrating here is Crysfire 2003, to be released very shortly in 16-bit and 32-bit versions (yes, 32-bit at last, though not yet GUI-based!).
These are (or will be) available free for non-profit use (and inexpensively for industrial users).
They’re aimed at making life easier for non-specialists in indexing (with some crystallographic knowledge).
Industrial Crysfire will be a graphical 32-bit version, more automated and aimed to be usable by technicians, who are not necessarily crystallographers. Hopefully it will be released early next year.

## Slide 14: A “Buyer’s Guide”: Some characteristics of the Indexing Programs now supported by Crysfire
Tolerates: Random
Program Impurities Errors Comments
Ito12 Yes No Optimised for low-symmetry
Fjzn6 Yes No As for Ito12, but more robust
Dicvol91 No Slows Good for screening to orthor./monoc.
Lzon Slows Slows Best for dominant-zone cases
Losh Slows Slows User-guided, faster than Lzon
Treor90 Yes No Specialises in v accurate impure data
Kohl [=TMO] Yes Yes Fast, useful for high & low symmetry
Taup [=Powder] Slows ?Slows Good for screening down to orthor.
Mmap No Yes Gives visual maps of solution space
Hmap Yes! Yes Gives visual joint-probability maps
McMaille Yes ?Slows Likely to need overnight runs

## Slide 15: How Much does Cell Volume Matter? (Can one index a protein?)
Formally the indexing problem is scale independent: it uses only relative dimensions and is unchanged if the d-spacings and wavelength are both doubled.
So why do large cells make indexing harder?
Although indexing is scale-independent, instrument resolution and accuracy are not, so if the d-spacings are 10 times bigger, the data must be 10 times better.
Also, classic programs like Ito & Treor were optimised for moderate cell volumes (i.e. below c.5000 A3).
Bob von Dreele has indexed several protein patterns, at least in high symmetry (and solved their structures).
Crysfire includes re-scaling to support this, as we’ll see.

## Slide 16: < Working with High Volume Datasets > 1) Crysfire: SC command Improving data via self-calibration 2) Crysfire: Indexing a Protein 3) Chekcell: LePage / Best Solution Seeking a higher-symmetry cell (Demonstration)

## Slide 17: Conclusions
The powder-indexing problem is now well understood (though not always solved, especially if you don’t use the right tools).
There are powerful indexing programs available and becoming more widely used (more in the pipeline - watch this space).
Crysfire offers easy access to 9 of them (from next month, Crysfire 2003 will make that 11).
Crysfire’s strength lies in finding trial cells, not in establishing their best description and symmetry.
That job is best done as a separate stage, using the graphical helper program, Chekcell.
Crysfire and Chekcell are complementary, and if used together are likely to offer the quickest route to success.
Even protein data can now be indexed (given very good data).

## Slide 18: Contributing Authors: Crysfire & Chekcell
Crysfire: Overall system + Mmap, Hmap, Lzon, Losh, etc
Robin Shirley
Contributed crystallographic software
Franz Kohlbeck Kohl [=TMO]
Armel Le Bail McMaille
Daniel Louër Dicvol, Losh, Lzon
Ton Spek & A. Meetsma Clepage
Daniel Taupin Taup [=Powder]
Arie van der Lee Eva2crys
Jan Visser Ito, Fjzn, Lzon, etc
Per-Eric Werner Treor
Chekcell
Jean Laugier & Bernard Bochu

## Slide 19: < Discussion >

## Slide 20: Classification of Indexing Methods
Method Space Exhaustive Status Program(s) available
Zone indexing Parameter No Mature Yes (2)
Successive dichotomy Parameter Yes/(semi) Mature Yes (2+)
Grid search Parameter Yes Semi-mature Yes (1)
Combined heuristic Parameter Semi Mature Yes (2)
Joint probability Parameter Semi Developing Yes (1)
Genetic algorithms Parameter No Developing Yes (1)
Monte Carlo Parameter No Semi-mature Yes (2)
Simulated annealing Parameter No Not yet tried No
Diffusion equation Parameter No Not yet tried No
Scan/covariance Par. (both) To monoc. Semi-mature Yes (1)
Index heuristics Index No Mature Yes (2)
Index permutation Index Yes Mature Yes (1)
(The list is not claimed to be complete. Only symmetry-general methods included)

## Slide 21: Methods vs Programs
Space Method Programs using this method
Parameter Zone indexing ITO12, FJZN6
Successive dichotomy DICVOL91, X-Cell,[LZON, LOSH]
Grid search SCANIX, Mmap, Hmap, (Powder49)
Combined heuristic LZON, LOSH, Mmap, Hmap
Joint probability Hmap
Genetic algorithms AUTOX, (W.P.G.A.: Harris...)
Monte Carlo McMaille, SVD-Index
Simulated annealing (not yet implemented)
Diffusion equation (not yet implemented)
Profile-based McMaille (idealised), (W.P.G.A.)
Par. (both) Scan/covariance EFLECH/INDEX
Index Index heuristics TREOR90, TMO [=KOHL]
Index permutation POWDER [=TAUP]
(Underlined if supported by Crysfire, in round brackets if not generally available)

## Slide 22: Indexing Programs: 1) Overview
Program Author(s) Method Space Exh. O/S
ITO12 Visser Zone index Par No DOS +?
FJZN6 Visser & Shirley Zone index Par No DOS
DICVOL91 Louër Dichotomy Par Mainly DOS +?
X-Cell Neumann Dichotomy Par Mainly Win
SCANIX Paszkowicz Grid search Par Yes DOS/ANSI
(Powder49) Shirley Grid search Par Semi Mainframe
LZON Shirley/Louër/Visser Comb. heur. Par Semi DOS
LOSH Shirley & Louër Comb. heur. Par Semi DOS
Mmap, Hmap Shirley Comb. heur. Par Semi DOS,Win
AUTOX Zlokazov Genetic alg. Par No DOS/extender
McMaille Le Bail Monte Carlo Par No Win
SVD-Index Coelho Monte Carlo Par No Win
(W.P.G.A.) Harris… Genetic alg. Par No Unix
EFLECH/INDEX Bergmann Scan/covar. P/(I) Mainly DOS,Win,Lin
TREOR90 Werner Index heur. Ind No DOS +?
TMO [=KOHL] Kohlbeck Index heur. Ind No DOS +?
POWDER [=TAUP] Taupin Index perm. Ind Yes DOS +?
(Underlined if supported by Crysfire, in round brackets if not generally available)

## Slide 23: Indexing Programs: 2) Performance (1GHz Pentium)
Program Orthor. Monocl. Tricl. Comments
ITO12 1 sec 1 sec 1 sec Automatic
FJZN6 2 sec 2 sec 2 sec Automatic
DICVOL91 <3 sec 1-30 min mins-hours Auto., v. vol.-dependent
X-Cell Variable: minutes-hours Automatic
SCANIX c.5 min (?5 min) n.a. User guided in monocl.
(Powder49) c.5 min in each case (PC Equiv.), user guided
LZON 30 sec - 5 min in each case Automatic
LOSH <30 sec <30 sec <30 sec User guided
Mmap, Hmap 10 sec - 15 min in each case User guided
AUTOX ?15 sec ?5 min ?30 min Semi-auto. in practice?
McMaille Variable: hours in black box mode Automatic
SVD-Index Variable: minutes-hours Automatic
(W.P.G.A.) Run times said to be lengthy (Alpha / SGI workstn.)
EFLECH/INDEX 3 min 15 min 5 min c.Auto, Exh. to monocl.
TREOR90 <30 sec <30 sec <30 sec Automatic
TMO [=KOHL] <30 sec <30 sec <30 sec Automatic
POWDER [=TAUP] <5 sec 15 min+ Very long Automatic
(Typical run times as a rough guide, but may vary considerably with data & settings)

## Slide 24: Indexing Programs: 3) Tolerance of impurities, etc
Tolerates: Random
Program Impurities Errors Comments
ITO12 Yes No Optimised for low-symmetry
FJZN6 Yes No As for ITO12, but more robust
DICVOL91 No Slows Good for screening to orthor./monoc.
X-Cell Yes Slows? Commercial package (Accelrys)
SCANIX Yes Slows? Under development, user guided
(Powder49) Slows Maybe Superseded by LZON
LZON Slows Slows Best for dominant-zone cases
LOSH Slows Slows User-guided, faster than LZON
Mmap Slows Maybe User-guided, good for dominant zones
Hmap Yes, very No User-guided, good for dominant zones AUTOX Slows? Slows? Many optional user settings
McMaille Yes Slows? Uses idealised whole profile
SVD-Index Yes Slows? Commercial package (Bruker)
(W.P.G.A.) Yes Slows Uses whole profile, developing
EFLECH/INDEX Yes Slows Uses full peak-fit covariance matrix
TREOR90 Yes No Specialises in v accurate impure data
TMO [=KOHL] Yes Yes Fast, useful for high & low symmetry
POWDER [=TAUP] Slows Slows? Good for screening down to orthor.
(Though nominally automatic, in practice AUTOX often needs some user guidance)